# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

## PRODUCT INFORMATION

## Product Description:

26-7R is a colored PVC Electrical Insulation Tape with a Rubber based adhesive, which is flame retardant and cold weather resistant used general for insulating, protection, and color-coded of electrical wires; for wire harnessing in automotive industry.

TECHNICAL DATA

PROPERTY Backing Plasticized PVC Adhesive Rubber based Total Thickness 7 Mil (0.18mm) Voltage Breakdown 8kv Peel Adhesion 16.4oz/in Tensile Strength 14.8 lbs/in Elongation at Break 200% Temperature Resistance 14ºF to +176ºF Core listed UL/CSA/CE COLORS AVAILABLE Black, Yellow, Green, Orange, Purple, White, Red, Blue, Gray & Brown

# Text boxes

26-7R

All Weather Colored Electrical Tape