The 2925 Series performs as a plasma or flame spray masking tape, allowing areas to be free of grit blasting and the plasma spray coating.  Its high-temperature resistance make it ideal for heat and reflectant tapes, and it is used in aerospace and automotive markets as a wire harness bundling tape in engine components.  Also, used as sound and vibration dampening product.

|  | 2925-7 | 2925-11 |
| --- | --- | --- |
| Backing Material | Glass-Foil | Glass-Foil |
| Adhesive Type | Silicone | Silicone |
| Total Thickness (in.) | .0070 | .0110 |
| Backing Thickness (in.) | .0025 | .0075 |
| Adhesive Thickness (in.) | .0045 | .0035 |
| Adhesion to Steel (oz./in.) | 60 | 75 |
| Tensile Strength (lbs./in.) | 130 | 200 |
| Elongation (% at break) | 7 | 7 |
| Operating Temperature (ºF) | -100 to 500 | -100 to 500 |
| Color | Aluminum | Aluminum |

Features:  High-temperature silicone adhesive allows the product to withstand continuous high temperatures, and prevents tape slippage after application.  Both have excellent strength and flexibility, which provides easy wrapping of complex shapes and minimizes wrinkling.