CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com PRODUCT INFORMATION

PRODUCT DESCRIPTION

Clear, translucent polycarbonate film with first surface velvet and a second surface matte.

PHYSICAL PROPERTIES:

PROPERTY TYPICAL VALUE UNITS TEST METHOD Specific Gravity ASTM D792 Conversion factor 160 ft²/lb-mil Water absorption (immersion @ 73ºF 24 hours) 0.33 % ASTM D5470 First surface gloss 80º angle, black inked second surface 3.0-4.5 Gloss unit ASTM D2457 First surface roughness R3Z 16-23 Microns ISO 4288 THERMAL PROPERTIES: PROPERTY TYPICAL VALUE UNITS TEST METHOD Heat deflection temperature ISO 75 1.82 mpa 270 ºF 0.45 mpa 288 ºF Vicat softening temperature 315 ºF ISO 306

MECHANICAL PROPERTIES:

| PROPERTY | TYPICAL VALUE | UNITS | TEST METHOD |
| --- | --- | --- | --- |
| Tensile strength, yield | 8,700 | Psi | ASTM D882 |
| Tensile strength, break | 8,600 | Psi | ASTM D882 |
| Elongation@break | 120 | $ | ASTM D882 |
| Tear strength, initiation | 1,100 | Lb/in | ASTM D1004 |

OPTICAL PROPERTIES:

| PROPERTY | TYPICAL VALUE | UNITS | TEST METHOD |
| --- | --- | --- | --- |
| Haze |  | % | ASTM D1003 |
| Light transmission | 90 | % | ASTM D1003 |
| Yellowness index | 1 |  | ASTM E313 |

# Text boxes

38-__F-VM

Polycarbonate Film

Velvet/Matte