CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 USA 70-Silicone

Silicone Coated Fiberglass

PRODUCT DESCRIPTION

Silicone coated fiberglass is engineered to retain the distinctive properties but by adding a glass fabric to the matrix, we are able to obtain the added benefits of dimensional stability, excellent tensile strength and extremely low elongation (<1%). USDA approval for food processing and handling, and FDA compliant (21 CFR177.1550). In addition, our materials operate in temperatures from -400°F (-240°C) under static conditions and -100°F (-73°C) under dynamic conditions up to 500°F (260°C). TYPICAL APPLICATIONS Shrink packaging – bundling Baking and cooking – Manufacturing of flavorants UV curing of wood products Tank seals and containment barriers – Gaskets, membranes, seals and diaphragms Protective curtains and aprons

Product ID Color Plys Friction Surface Nominal Thickness Weight (lbs/sq. yd.) Tensile Warp (lbs/sq. in.) Tensile Fill (lbs/sq. in.) Recommended Min. Pulley Dia. Maximum Widths (in.) 70-10R Red 1 N .010" 0.62 120 100 3" 38* 70-15R Red 1 N .015" 0.87 250 200 3" 38* 70-18R Red 1 N .018" 1.05 525 375 3" 38* 70-20R Red 1 Y .020" 1.15 525 375 3" 50* 70-25R Red 1 N .025" 1.44 525 375 3" 50* 70-42R Red 2 Y .042" 2.05 1050 750 3" 50* 70-62R Red 3 Y .060" 3.07 1575 1125 3" 50* 70-10W White 1 N .010" 0.62 120 100 3" 38* 70-15W White 1 N .015" 0.87 250 200 3" 38* 70-18W White 1 N .018" 1.05 525 375 3" 38* 70-20W White 1 Y .020" 1.15 525 375 3" 50* 70-25W White 1 N .025" 1.44 525 375 3" 50* 70-42W White 2 Y .042" 2.05 1050 750 3" 50* 70-62W White 3 Y .060" 3.07 1575 1125 3" 50*