# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

PRODUCT INFORMATION

## Product Description:

# High Strength grade silicone sheeting is used in applications where high strength physical properties are needed; with very high tear resistance and a high tensile strength.  The material is also listed in CFR 177.2600 – this FDA regulation deal with rubber articles intended for repeated use in contact with food.  Material is also ozone and UV resistant.

Common Applications:

Excellent Gasketing Material – used in Extreme high and low temperatures.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.18 |
| Durometer, Shore A | ASTM D2240 | 60 +/- 5 |
| Tensile Strength, psi | ASTM D412 | 1275 |
| Elongation, % | ASTM D412 | 500 |
| Tear, psi Die “B” | ASTM D624 | 190 |
| Temperature Range | ºF | -94 to +450ºF |

ZZR-765 CL3B GR 60

ASTM D2000

# Text boxes

Extreme High Strength

Silicone Sheeting,

60 Shore “A”

71-HS