# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

## Product Description:

# Fiberglass reinforced silicone sheet is typically used in gasket or seal applications.  Material is resilient, non porous and suitable for operating in temperatures from -100 to +500ºF but is not limited to such applications.  Fiberglass Reinforced Silicone is resistant to deterioration by weathering and engine oil it remains flexible [-100 to +500ºF] and is available in many different thicknesses.  The fiberglass is centered between 2 layers of silicone that gives the material dimensional stability and higher tensile strength.

Common Applications:

# Fiberglass reinforced press pad material is typically used for flexible circuitry laminations.  This process requires a resilient, non-porous sheet material suitable for operating temperatures from -100 to 500F.  It can also be used for gaskets, diaphragms, and belting.

### TYPICAL PROPERTIES

| Property | Silicone Rubber |
| --- | --- |
| Durometer, Shore A | 70 +/-10 |
| Fiberglass Thickness | .014” |
| Weight (oz per sq. yd.) | 12.5 |
| Break Strength (warp/fill), psi | 400 x 350 |
| Plain Weave Thread Count | 20 x 18 |
| Diaphragm Burst Strength, psi | 750 |
| Compression Set % | 35 max |
| Temperature Range ºF | -100 to +500 |

SPECIFICATIONS:

AMS3320

AMS3315

# Text boxes

Fiberglass Reinforced Silicone Sheet

71-REF