# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

# PRODUCT INFORMATION

## Product Description:

# Specification Grade silicone sheeting is designed to be used in applications where higher physical properties are required.  Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless, chemically inert and non-toxic.  It offers all FDA approved ingredients, low compression set and fungus resistance.

Common Applications:

# Silicone rubber can be used for insulating and cushioning electronic assemblies.  It is also used for gaskets, automotive seals and hoses, shaft sealing rings, spark plug caps, vibration and sound damping, industrial rollers, press pads, thermal shielding, food and cosmetic services, heat sealing and packaging and grommets.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.45 |
| Durometer, Shore A | ASTM D2240 | 50 +/- 5 |
| Tensile Strength, psi | ASTM D412 | 850 |
| Elongation, % | ASTM D412 | 400 |
| Tear, psi Die “B” | ASTM D624 | 120 |
| Temperature Range | ºF | -80 to +500 |

Available Industry Specifications:

ZZR-765 CL2A & 2BGR50, AMS 3302, ASTM D2000

# Text boxes

Specification Grade  Solid Silicone Rubber,

50 durometer