# CS Hyde Company                               PRODUCT INFORMATION

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046						10- S Series

## Product Description:

UHMW is a super tough, abrasion resistant material.  It has a high-slip/ non-stick surface similar to that of Teflon® but UHMW can take eight times the abrasion than that of Teflon® coated fiberglass and it is also very cost efficient.  The 19 Series also has a low coefficient of friction and good chemical/ stress cracking resistance.  Since UHMW is such a versatile material, it can be used in all industries.

Performance & Application Information:

UHMW is ideal in situations that deal with friction, corrosion, sliding, noise reduction, wear, sticking, gliding, and surface protection.  Examples of applications include:  chute liners and wear strips on conveyor systems, top surface on snowboards, skateboards, gaskets, washers, rails, shims, chain guides, buzz, and squeak and rattle noise reduction in the automotive industry, door glides, sliding surface on router tables and many more.

### TYPICAL PROPERTIES

|  | 19-3R | 19-5R | 19-10R |
| --- | --- | --- | --- |
| UHMW Thickness (in.) | .003 | .005 | .010 |
| 8345* Rubber Adhesive (in.) | .0053 | .0053 | .0053 |
| Total material thickness (in.) | .0083 | .0103 | .0153 |
| Adhesion (oz./in.) | 90 | 90 | 90 |
| Elongation (%) | 300 | 300 | 300 |
| Tensile Strength PSI | 6000 | 6000 | 6000 |
| Dielectric Strength | 3,000 | 3,000 | 3,000 |
| Coefficient of Friction | 0.2 | 0.2 | 0.2 |
| Temperature Rating (cont.) | 0ºF to 120ºF |

*Avery 8345 standard adhesive w/ 175 oz./in. peel strength and temperature range of 120ºF-175ºF, very aggressive, bonds well to metal, painted surfaces and many other low surface energy materials that require high tack.

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.  Teflon® is a registered trademark of DuPont.

# Text boxes

19-R  Series

UHMW Polyethylene Film with Rubber Adhesive