# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

# PRODUCT INFORMATION

## Product Description:

The Premium Grade fabric series is a multi-purpose material that has a slick, non-stick surface.  This material is constructed of a PTFE (Teflon®) coated woven fiberglass substrate.  The 50-X Series exhibits exceptional release properties and high resistance to heat, chemicals and moisture.  PTFE fluorocarbon resin is one of the most chemically inert materials available. It is also highly resistant to wear, tear, cut through and breakage, even under conditions of extreme temperature and pressure.

Performance & Application Information:

These products are designed for applications requiring a quick release/non-stick surface and/or high operating temperatures (-240ºF to 500ºF).  Applications include: heat sealing platen and element covers, lamination release covers, shrink wrapping, blister packing, plastic bag manufacturing, chute liners, commutator insulation, slot liners, cable & conductor wrapping and many more.

### TYPICAL PROPERTIES

|  | 50-3X | 50-5X | 50-6X | 50-10X | 50-13X |
| --- | --- | --- | --- | --- | --- |
| Nominal Thickness (in.) | .003 | .005 | .006 | .010 | .013 |
| Nominal Weight (oz./yd²) | 4.4 | 8.0 | 9.40 | 15.9 | 20.0 |
| Dielectric Strength (volts/mil) | 900 | 1100 | 1200 | 900 | 500 |
| Resin Content (%) | 68 | 61 | 67 | 62 | 58 |
| Breaking Strength Warp (lbs./in.) | 60 | 140 | 150 | 225 | 350 |
| Breaking Strength Fill (lbs./in.) | 50 | 140 | 150 | 175 | 250 |
| Trapezoidal Tear Warp (lbs.) | 2 | 4 | 4 | 10 | 10 |
| Trapezoidal Tear Fill (lbs.) | 1 | 4 | 4 | 8 | 10 |

# Text boxes

50-X Series

PTFE (Teflon®) coated fiberglass fabric