CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com PRODUCT INFORMATION

A woven lightweight fabric of an Aramid fiber blend over a fiberglass core yarn. Applications include safety clothing, curtains, heat shields, filtration cloth, and rubberized hose. Resistant to reflective heat sources. Offers good thermal protection for safety garments.

Specifications				8 oz.			17 oz.			30 oz.

Base Fabric		     		Aramid/Fiberglass        	Aramid/Fiberglass     	Aramid/Fiberglass

Color/Appearance			Yellow			Yellow 			Yellow

Available Widths			40”			36” thru 60”		40”

Roll Length				50 yds.			50 yds.			50 yds.

Weave Style				Plain			Plain			Plain

Construction(ends x picks)		20 x 17/in²		20 x10.5/in²		31 x 14/in²

Fabric Weight				8.3 oz/yd²		17 oz/yd²		30oz/yd²

Fabric Thickness			0.027”			0.057”			0.110”

Warp Strength				125 lbs/in		282 lbs/in		370 lbs/in

Fill Strength				120 lbs/in		130 lbs/in		230 lbs/in

Abrasion Resistance			Excellent		Excellent		Excellent

Thermal Conductivity (k)		.360			.441			N/A

(Btu x in/hr x ft² x ºF)			(ASTM D2214-70)	(ASTM C-177)       	 (ASTM C-177)

Total Conductance (c)	12.00		8.700			N/A

(Btu/hr x ft² x ºF)			(ASTM D2214-70)	(ASTM C-177)        	(ASTM C-177)

Total Resistance (r)			.083			.115			N/A

(hr x ft² x ºF/btu)			(ASTM D2214-70)	(ASTM C-177)       	 (ASTM C-177)

Coating Certifications	N/A			N/A			N/A

Solvent &

Chemical Resistance			Good			Good			N/A

Sunlight &

Age Resistance				UV sensitive		UV sensitive		UV sensitive

Electrical Properties			N/A			N/A			N/A

# Text boxes

60- SERIES

Aramid/Fiberglass

Fabric