Silicone rubber coated fiberglass fabric. Superior release characteristics, particularly with sticky substances. From thin (010" thick) to thick (.062" thick). Available in 1, 2 and 3 ply. Red or White Color. Silicone Coated Fabric can be custom made into continuous loop silicone BELTS for conveyance in Food & Packaging industries. Used as flaps in shrink tunnels, can be die cut into gaskets, strips, washers, insulators

Technical Data:

Substrate					Woven Fiberglass

Coating						Silicone (wash coat one side)

Nominal Thickness:				.020”	ASTM D-374

Weight (Lbs/sy. Yd.)				1.15	ASTM D-3376

Elemdorf Tear Warp:				>6400 grams ASTM-1424

Elemdorf Tear Fill:				>6400 grams ASTM-1424

Breaking Strength -Warp (lbs/sq inch):		525	ASTM D-902

Breaking Strength - Fill (lbs/sq inch):		375	ASTM D-902

Color:						Silicone “Red”

Tolerance Width  +/- 1/8”