# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

## Product Description:

# FDA grade silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance. This material is low volatile, peroxide free and does not discolor over time Silicone is odorless, tasteless, chemically inert and non-toxic.  It offers all FDA approved ingredients, low compression set and fungus resistance.

Common Applications:

# Silicone rubber can be used for insulating and cushioning electronic assemblies.  It is used for LCD displays, sensors for lasers and assemblies, gaskets, automotive seals and hoses, shaft sealing rings, spark plug caps, vibration and sound damping, industrial rollers, press pads, thermal shielding, food and cosmetic services, heat sealing and packaging and grommets.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.45 |
| Durometer, Shore A | ASTM D2240 | 50 +/- 5 |
| Tensile Strength, psi | ASTM D412 | 700 |
| Elongation, % | ASTM D412 | 300 |
| Tear, psi Die “B” | ASTM D624 | 40 |
| Temperature Range | ºF | -103 to +450 |

Available Industry Specifications:

CFR 177.2600, ASTM D2000

# Text boxes

FDA Grade

Solid Silicone Rubber,

50 durometer