CS Hyde Company

1351 N. Milwaukee Ave.

Lake Villa, IL  60046

Ph. 847/395-0325

Fax 847/395-0334

Series THTQ-14 & THTQ-17

Teflon coated Quartz thread is a manufactured thread from high purity, very fine continuous filament pure fused silica, making it among the strongest and most temperature and chemically resistant thread on the market today. Our proprietary PTFE coating process completely encapsulates the thread, enhancing resistance to buildup of contaminants and repelling attack by most acids and alkalis. This sewing thread will not support combustion and will not burn. In addition, our proprietary coating process penetrates further and coats each fiber bundle more completely, improving handling characteristics and abrasion resistance versus other’s Quartz sewing thread.  Operating Temp: 2000ºF, PTFE Coating 600ºF

Features

Extreme Temperature Resistance

High Strength

Chemical Resistance

Proprietary Coating Process

Uniform PTFE coating

Balanced Twist

Benefits

Chemical Resistance

Minimize Buildup of Contaminants

Maximum Fiber Bundle PTFE Penetration

Good Sewability

Excellent Thermal Shock Resistance

Flexibility

Minimize strip-back and untwisting

| Product Number | THTQ-14 | THTQ-17 |
| --- | --- | --- |
| Thread Style | Continuous Filament Pure Fused Silica | Continuous Filament Pure Fused Silica |
| Coating Type | PTFE, Sintered | PTFE, Sintered |
| Coating Percentage | 20 | 20 |
| Yield (yd/lb. nom.) | 2950 | 1975 |
| Tensile Strength (lbs) | 12 | 20 |
| Diameter (nom. Inches) | .014 | .017 |
| Final Twist | “Z” | “Z” |
| Color | Natural / Tan | Natural / Tan |