CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com PRODUCT INFORMATION

PRODUCT DESCRIPTION

UHMW is a super tough, abrasion resistant material. It has a high-slip/ non-stick surface similar to that of Teflon® but UHMW can take eight times the abrasion than that of Teflon® coated fiberglass and it is also very cost efficient. The UHMW film provides an excellent low friction, non-stick surface, in many ways similar to PTFE. The 19-A series is pressure sensitive with an aggressive permanent acrylic adhesive

APPLICATION INFORMATION

The 19-A series is used primarily in mechanical applications such as chute liners, wear pads, and guide rails. It can also be used in such applications as a glide surface for computer mouse. The acrylic transfer adhesive has a temperature range of 225ºF – 300ºF. Excellent UV, temperature, moisture and chemical resistance. Very versatile.

TECHNICAL DATA

Test Method 19-3A 19-5A 19-10A 19-20A Backing Thickness (in.) .003 .005 .010 .020 Adhesive Thickness (in.) .002 Adhesion Acrylic Elongation (%) ASTM-D 882 300 Tensile Strength (psi) ASTM-D 882 6000 Dielectric Strength (V/mil) ASTM-D 149 3000 Thermal Conductivity (73)[(BTUin)/(ft²hrºF)] 0.44 Temperature Range (cont.) 0ºF to 200ºF Water Absorption .01 Density (g/cc) .93 Heat Distortion (ºF) ISO R75 Method A 203 Coefficient of Thermal Expansion ~1.1x104 Deformation (%) 2000 psi, 6hr.,122ºF 6-8 Dissipation Factor ASTM-D 150 0.0004

Width:		25” up to 24”

Length:          18 (or) 36 yards

# Text boxes

19-__A

UHMW Film w/

Acrylic Adhesive