CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com PRODUCT INFORMATION

PRODUCT DESCRIPTION

Polysulfones (PSU) are tough, rigid, high-strength thermoplastics that are suitable for continuous use up to 300ºF (149ºC). The resins are resistant to oxidation and hydrolysis and withstand prolonged exposure to high temperatures and repeated sterilization. Polysulfones are highly resistant to mineral acids, alkali and salt solutions. Their resistance to detergents and hydrocarbon oils is good, but they will be attacked by polar solvents such as ketones, chlorinated hydrocarbons, and aromatic hydrocarbons. PSU’s are also highly resistant to degradation by gamma or electron beam radiation. Electrical properties of polysulfones are stable over a wide temperature range and after immersion in water or exposure to high humididty. Applications of PSE films are mainly in electronics, CPI and automotive.

PHYSICAL PROPERTIES:

TEST METHOD SI UNITS US CUSTTOMARY UNITS Glass Transition Temp. ASTM D-3418 190 ºF 374 ºF Water Absorption ASTM D-570 0.3 % 0.3 % @ 50ºC (122ºF), 75%RH, 24 hrs Yield Internal 753 m²/kg/µm 20,833 in²/lb/mil MECHANICAL PROPERTIES MD – TD MD - TD Stress at Yield @ 23 ºC (73ºF) ASTM D-882 68 MPa - 63 MPa 9,90psi - 9,200 psi Elongation at Yield @ 23 ºC (73ºF) ASTM D-882 5 % - 5 % 5 % - 5% Stress at Break @ 23 ºC (73 ºF) ASTM D-882 59 MPa - 57 MPa 8,500 psi - 8,200 psi Elongation at Break @ 23 ºC (73 ºF) ASTM D 882 55 % - 35% 55 % - 35 % Modulus @ 23 ºC (73 ºF) ASTM D-882 2310 MPa - 2340 MPa 335 kpsi - 340 kspi Dart impact ASTM D-1709 399 g 0.88 lb Tear Propagation ASTM D-1922 12 gforce - 12 gforce 0.026 if - 0.026 lbf Tear Resistance ASTM D-1004 960 gforce - 970 gforce 2.13 lbf - 2.14 lbf ELECTRICAL PROPERTIES Dielectric Strength ASTM D-149 3,200 V/mil *Reported values were measured on a 30µm thick film

# Text boxes

34-__F

UDEL / PSU Film