CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com PRODUCT INFORMATION

PRODUCT DESCRIPTION

Clear general purpose polycarbonate film that delivers superior impact and clarity. APPLICATIONS: Automotive, Labels, Membrane Switches, Nameplates, Packaging

PHYSICAL PROPERTIES:

PROPERTY TYPICAL VALUE UNITS TEST METHOD Specific Gravity 1.2 ASTM D792 Conversion Factor 160 ft²/lb-mil Water Absorption (Immersion @ 73ºF 24 hrs.) 0.33 % ASTM D570 First Surface Gloss- 60º angle, black inked second surface ≥98 Gloss unit ASTM D2457 First Surface Roughness R3Z ≥0.5 Microns ISO 4288 THERMAL PROPERTIES: PROPERTY TYPICAL VALUE UNITS TEST METHOD Heat Deflection Temp. ISO 75 1.62 Mpa 270 ºF 0.45 Mpa 288 ºF Viscat Softening Temp. 315 ºF ISO 306 OPTICAL PROPERTIES: PROPERTY TYPICAL VALUE UNITS TEST METHOD Haze 0.3 % ASTM D1003 Light transmission 91 % ASTM D1003 Yellowness index 1 ASTM E313

MECHANICAL PROPERTIES: PROPERTY TYPICAL VALUE UNITS TEST METHOD Tensile Strength, Yield 8,800 Psi ASTM D882 Tensile Strength, Break 8,700 Psi ASTM D882 Elongation @ Break 120 % ASTM D882 Tear Strength, Initiation 1,100 Lb/in ASTM D1004

# Text boxes

38-__F-GG

Polycarbonate Film

Gloss/Gloss