CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com PRODUCT INFORMATION

PHYSICAL PROPERTIES:

Property Test Method Units Value Mechanical Tensile Stress ISO 8256 kJ/m2 300 Strain 10% Strain 5% Yield Stress ISO 527-1/2 MPa 50mm/min 30 Stress at Break ISO 527-1/2 MPa 45,8 Nominal Strain at Break ISO 527-1/2 % 50mm/min >50 Strain at Break ISO 527-1/2 % 360 Yield Strain ISO 527-1/2 % 50mm/min 25 Tensile Modulus ISO 527-1/2 MPa 1mm/min 525 Tensile Creep Modulus ISO 899 MPa 1000h 312 1h 360 Flexural Modulus ISO 178 MPa -40C 2410 23C 570 100C 207 Notched Izod Impact ASTM D 256/A J/m -40C 40 23C 210 Notched Charpy Impact ISO 179/1eA kJ/m2 -30C 5 23C 30 Unnotched Charpy Impact ISO 179/1eU kJ/m2 -30C No break 23C No break

# Text boxes

46-__F

HYTREL 7246 FILM