# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

PRODUCT INFORMATION

## Product Description:

# Electrically Conductive Grade silicone sheeting is designed to be used in many different applications.  It is black; carbon filled silicone sheeting that will act as a low amperage conductor and provide protection against electrostatic discharge.  Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless, chemically inert and non-toxic.  It offers low compression set and fungus resistance.

Common Applications:

# Silicone rubber can be used for insulating and cushioning electronic assemblies.  It is also used for gaskets, heat sealing and packaging, RFI/EMI Shielding.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.30 |
| Durometer, Shore A | ASTM D2240 | 70 +/- 5 |
| Tensile Strength, psi | ASTM D412 | 700 |
| Elongation, % | ASTM D412 | 200 |
| Tear, psi Die “B” | ASTM D624 | 80 |
| Temperature Range | ºF | -80 to +500 |
| Volume Resistivity | (ohms/cm) | 6 |

UL94 HB Rated for 1/32”+ Thickness

# Text boxes

Electrically Conductive Grade

Solid Silicone Sheeting,

70 Shore A