# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

# PRODUCT INFORMATION

## Product Description:

# Thermally conductive silicone is an unsupported thermally conductive solid silicone rubber.  This is a filled silicone rubber material that does not require curing and it is formulated to provide clean release from most surfaces.  This material is rigid enough to be easily die-cut and the gap filler can readily be repositioned.  The 71-TCD series is offered to fill the needs of an unsupported thermal transfer material in applications requiring clean release and enhanced thermal performance by filling air gaps and electrical isolation.

Common Applications:

This material offers thermal conductivity along with electrical isolation for heat transfer applications between PC boards and Heat Sinks.  It can also be used to fill air gaps between PC boards and heat sinks.  Thermally conductive silicone can also be used in electronic modules for power devices for power supplies, computers, telecommunication, automotive electronics, electrical insulation, military, medical, heat pipe assemblies, and CD ROM cooling.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Color | Visual | Light Blue |
| Thermal Conductivity | ASTM E1530 | 1.3 |
| Thermal Impedance (ºC in.²/W) (1/16”) | ASTM E1530 | 1.25 |
| Break Strength (psi) | ASTM D412 | 250 |
| Elongation (%) | ASTM D412 | 200 |
| Hardness (Shore A) | ASTM D2240 | 65 |
| Dielectric Strength (volts/mil) | ASTM D149 | 250 |
| Volume Resistivity (ohm-cm) | ASTM D257 | 5 x 10 15 |
| Operating Temp (ºF) |  | -80 to 400 |
| UL Listing Recognition | UL94 | HB |

# Text boxes

71-TCD

Thermally Conductive Solid Silicone Rubber,

70 durometer