# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

## Product Description:

# Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless and non-toxic.  It offers high compressibility with a low compression set.  Flame retardant silicone sponge is black, dark blue / grey color and has a fine fabric finish on both sides.

Common Applications:

# Silicone sponge can be used for insulating and cushioning electronic assemblies.  It can also be used for gaskets, seals, air filters, thermal shielding, cushioning for aviation, automotive and locomotive industries as well as flame-retardant applications.  This silicone sponge can also be used in furnace or boiler rooms, electrical boxes, high heat, high intensity lighting and after burners.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Foam |
| --- | --- | --- |
| Density, lbs/cubic in. under ¼” thick | ASTM D297 | .020 |
| Density, lbs/cubic in. over ¼” thick | ASTM D297 | .018 |
| Compression Deflection | ASTM D1056 | 6-14 psi |
| Compression Set | ASTM D1056 | 15 |
| Brittle Point |  | -103ºF |
| Temperature Range |  | -103 to +450 |
| Water Absorption | ASTM D1056 | Pass |
| Tensile Strength | ASTM D412 | 90 |
| Elongation | ASTM D412 | 150 |
| Flame Resistance | UL 94 | HB |

Available Industry Specifications:

DMS1980, UL 94HB

# Text boxes

###### Flame Retardant Medium Density

###### Silicone Sponge