# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

Lake Villa, IL  60046

PRODUCT INFORMATION

## Product Description:

# Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, high tensile strength, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless and non-toxic.  It offers high compressibility with a low compression set.

Common Applications:

# Fiberglass reinforced silicone sponge is an excellent material for gasketing applications.  The fiberglass gives it dimensional stability, which also helps in cutting close tolerance parts.  Fiberglass Reinforced Silicone sponge can be used for insulating and cushioning electronic assemblies.  It can also be used for gaskets, seals, belting, air filters, and diaphragms, thermal shielding.  This silicone sponge can also be used in furnace or boiler rooms, electrical boxes, high heat, high intensity lighting and after burners.

### TYPICAL PROPERTIES

| Property | Test Method |  |
| --- | --- | --- |
| Density (lbs./in.^3) | ASTM D297 | .025 max |
| Compression Deflection | ASTM D1056 | 9-18 psi |
| Compression Set % | ASTM D1056 | 25 |
| Temperature Range |  | -103 to +450 |
| Water Absorption % | ASTM D1056 | 5 max |

# Text boxes

###### Fiberglass Reinforced Medium Density

###### Silicone Sponge

###### 72-REF