CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 USA 800-461-4161 / Fax: 847-395-0535 www.cshyde.com / sales@cshyde.com 7-200A

Strip-N-Stick® Tape

PRODUCT DESCRIPTION

This tape is a silicone sponge with an aggressive acrylic adhesive. It offers the compressibility of a medium compression closed cell sponge with an acrylic pressure sensitive adhesive on one side. It is odorless, non-corrosive and non-toxic.

APPLICATION INFORMATION

Strip-N-Stick® Tape offers superior service life, excellent conformability, and flexibility. Other benefits include low compression set and high adhesion to a variety of substrates. Often chosen for high and low temperature resistance, gasketing, vibration dampening, and thermal insulation.

TECHNICAL DATA

PROPERTY DATA Thickness Available (inches) 1/16”, 3/32”, 1/8”, 3/16” Adhesive Type Acrylic Adhesion (oz/in.) 30 Tensile Strength (lbs./in.) 65 Elongation (%) 150 Compression Deflection (comp.75% of original) 10 Compression Set % (50% compression, 22 hrs. @ 212ºF) 25 Temperature Range (ºF) -20 to +325