CS Hyde Company

1351 N. Milwaukee Ave.

Lake Villa, IL  60046

Ph. 847-395-0325 Fax 847-395-0334

Braided PTFE Coated E-Glass Lacing Tapes and Tie Cords

| Product number | LT-779-18 | LT-779-15 | LT-779-13 | LT-779-11 | LT-779-7 | LT-761-.027 | LT-761-.034 | LT-761-.047 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Coating Type | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered | PTFE Unsintered |
| Braid Type | Flat | Flat | Flat | Flat | Flat | Round | Round | Round |
| Yield (yds/lb) | 220 | 325 | 430 | 520 | 1025 | 1550 | 540 | 360 |
| Thickness | .018 | .015 | .013 | .011 | .007 | n/a | n/a | n/a |
| Width (in.) | 1/8 | 7/64 | 5/64 | 3/32 | 3/64 | n/a | n/a | n/a |
| Diameter (in.) | n/a | n/a | n/a | n/a | n/a | .027 | .034 | .047 |
| Tensile (lb/min.) | 150 | 125 | 60 | 90 | 40 | 80 | 75 | 80 |

Lacing tapes are well suited for most applications requiring lacing tape (flat braid) or tie cord (round braid) to operate at extreme temperatures and in chemically aggressive environments. These tapes will not burn or support flame and will not rot or support fungus. In addition, our braided products are PTFE impregnated prior to braiding, thus increasing flexibility and knot strength versus other competitive products that are braided first, then PTFE coated. Our process yields a product that does not tend to shed loose glass filaments and remains flexible over time.  Applications include: commercial aircraft, military aircraft, municipal transportation, tying wire bundles, tying cable bundles and wire harnesses.

Features/ Benefits

High Temperature Resistance

High Strength

Uniform PTFE coating

Each Yarn Individually Coated

Excellent Flexibility

Chemical Resistance

Minimal Buildup of Contaminants

Excellent Knot Strength

Excellent Thermal Shock Resistance

Will Not Burn or Support Flame

Applicable Specifications:

E779-303… Mil-T-43435B, T4, Finish D

E761-1330… Mil-C-20079H, T3, Class 4

Martin…… STM-F-411, STM-F-417,

STM-F-420

Lockheed … 25-4066A

Boeing …. BAC 5107, BAC 5157

Hamilton Standard… 539769

General Electric…… 932A224

US Naval Command. 17773A11181007X

Elongation of lacing tape and tie cord is typically less than 5%. Operating Temps. 550 deg. F continuous

Colors other than natural may require minimum purchase quantity. Please consult the factory.

Dimensions shown are nominal, however most are within 10%. Consult factory as needed.

All values are typical and should not be used for specifications.