# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

## Product Description:

# Fluorosilicone silicone sheeting is designed to be used in applications where extreme temperatures exist.  Fluorosilicone silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance. Silicone is odorless, tasteless, chemically inert and non-toxic.  Fluorosilicone is resistant to harsh chemicals, fuels, oils and solvents.

Common Applications:

# Silicone rubber can be used for insulating and cushioning electronic assemblies.  It is used gaskets, seals, vibration mounts, thermal shielding and grommets.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.45 |
| Durometer, Shore A | ASTM D2240 | 60 |
| Tensile Strength, psi | ASTM D412 | 900 |
| Elongation, % | ASTM D412 | 200 |
| Tear, psi Die “B” | ASTM D624 | 40 |
| Temperature Range | ºF | -65 to +450 |
| Volume Change Fuel “C” 22 hrs @ 77ºF % |  | 20% |

Available Industry Specifications:

MIL-R-25988 TY2 Cl1 GR60, AMS3325

# Text boxes

Fluorosilicone

Solid Silicone Rubber,

60 durometer