CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 18-2A-WP

2 mil. White Polyimide Tape

PRODUCT DESCRIPTION

18-2A-WP is composed of a top coated matte white polyimide film and a aggressive permanent acrylic adhesive backed with a 50# kraft release liner.

APPLICATION INFORMATION

Ideal for marking electronic components, and the topside of through-hole printed circuit boards. Other applications include rating plates, nameplates, and industrial bar code applications requiring durability. This high-performance material is designed for applications requiring excellent solvent and scratch resistance.

TECHNICAL DATA Color Glossy white Adhesion Type Acrylic Backing Thickness (mils) 2 Total Tape Thickness (mils) 3.5 Adhesion to Steel: Oz/inch 25 Tensile Strength (lbs/inch) 50 Elongation: % 60 Dielectric Strength, Volts 11000

Service Temperatures: 1-20 Minutes 572°F/ 300°C 2-4 Minutes 617°F/ 325°C 1-9 Seconds 842°F/ 450°C 1-3 seconds 1000°F/ 538°C Minimum Application Temp. 50°F Exterior Durability: Indoors only Storage Stability: Store at 70°F and 40-50%RH Shelf Life 2 years at proper storage conditions

*The above values are "Typical Values" which have a nominal range about them and are not intended for specification purposes.

FOR ADDITIONAL INFORMATION PLEASE CALL CS Hyde Company 800-461-4161