# CS Hyde Company                             PRODUCT INFORMATION

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## Product Description:

Metalized Polyester Film tape is 0.9 mil. Thick with brilliant, vibrant mirror-like finish; coated with an aggressive long last acrylic adhesive system.  Tapes have an excellent chemical and thermal stability.  Silver can be qualified to meet Federal Specification #L-T-100B, Type II>

Performance & Application Information:

Reflective shielding, industrial and graphic arts, decorative trim, automotive trim, nameplates, electric appliances, advertising displays, suitable for microfilm splicing, also can be used in photo sensing applications to detect splices and to facilitate roll changeovers.

Available colors: Silver, Gold, Black, Red, Blue and Green 72 yds/rl.

### TYPICAL PROPERTIES

| Total thickness (in.) | 2.1 mil. |
| --- | --- |
| Adhesive | Acrylic |
| Adhesion to steel (oz/in) | 45 |
| Tensile strength (lb./ in. width) | 24.5 |
| Elongation (at break) | 100% |
| Water vapor transmission rate | 0.058gm/100in²/24 hr |
| Temperature | Up to 302ºF |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.

# Text boxes

24-MF

Metalized Polyester

Film Tape w/ Acrylic

Adhesive