# CS Hyde Company                              PRODUCT INFORMATION

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## Product Description:

The Porous Fabrics are specially formulated to be “breathable”, while at the same time, maintaining their unique non-stick properties.  These fabrics are manufactured from woven fiberglass substrates that have been coated with PTFE.  The Porous Fabrics possess controlled porosities that allow products to cure and outgas through the fabric.  Because of their unique properties, these fabrics are excellent for use in a wide variety of applications, from the manufacture of polymers to a release medium for composite molding.

Performance & Application Information:

These fabrics are engineered to retain the distinctive properties of PTFE; however, by adding a glass fabric to the matrix it is able to obtain the added benefits of dimensional stability, durability, and excellent tensile strength.  Typical applications include:  Manufacture of silicone rubber sheet, curing rubber & plastic foams and sponge, insulation and protection, composite mold release, release sheets for fabricating glass-resin structures

### TYPICAL PROPERTIES

|  | 56-3 | 56-5 | 56-10 | 56-14 | 56-25 | 56-28 |
| --- | --- | --- | --- | --- | --- | --- |
| Nominal Thickness (in.) | .003 | .005 | .010 | .014 | .025 | .028 |
| Nominal Weight (lb./yd²) | .13 | .26 | .48 | .70 | 1.30 | proprietary |
| Tensile (lbs./in.) | 56 | 100 | 200 | 320 | 520 | proprietary |
| Edge Tear Warp (grams) | 32 | 112 | 160 | 232 | 472 | >6400 |
| Edge Tear Warp (grams) | 380 | 800 | 1400 | 3700 | >6400 | >6400 |
| Edge Tear Fill (grams.) | 250 | 700 | 1100 | 3200 | >6400 | >6400 |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.  Teflon® is a registered trademark of DuPont.

# Text boxes

56 Series

Semi-Porous PTFE (Teflon®) coated fiberglass fabric