Product THT-Series is PTFE coated Beta (BC) fiberglass

sewing thread from manufactured from continuous filament beta yarns, making it

among the strongest and most chemically resistant textile sewing

thread on the market today. Our uniform PTFE coating completely

encapsulates the thread, enhancing resistance to build-up of contaminates

and repelling attack by most acids and alkalis. Our

smooth PTFE coating enhances the flexibility of this very fine fiberglass

yarn, making it especially suitable for most industrial sewing

machines and minimizing the tendency to kink, strip-back or

break like many other very high temperature threads. This is our

most popular, versatile and cost effective high temperature thread.

PTFE Coated Beta (BC) Fiberglass Sewing Thread

Features

High Temperature Resistance

High Strength

Uniform PTFE coating

Finest Glass Fiber Available

Excellent Flexibility

Benefits

Chemical Resistance

Minimal Buildup of Contaminants

Good Sew ability

Excellent Thermal Shock Resistance

Flexibility

Minimal strip-back and untwisting

Applications:

High Temperature Textiles

Safety Spray Shields

Filter Bags

Braided Sleeving

Insulation Jackets

Thermal Insulation Pads

High Temperature Gaskets

Kiln Seals

Fire Resistant Composites

Welding Blankets

Heat Shields

Product Data

| Product | THT-14 | THT-17 | THT-21 |
| --- | --- | --- | --- |
| Coating type | PTFE, Sintered | PTFE, Sintered | PTFE, Sintered |
| Coating % | 12 | 12 | 12 |
| Yield (yds/lb) | 3000 | 2000 | 1500 |
| Tensile (lbs) | 12 | 18 | 25 |
| Diameter (nominal) | .015” | .018” | .021” |
| Style | Beta/BC Fiberglass | Beta/BC Fiberglass | Beta/BC Fiberglass |
| Color | Tan | Tan | Tan |
| Operating Temp (F) | 600F | 600F | 600F |