# CS Hyde Company                               PRODUCT INFORMATION

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## Product Description:

# Low Compression Set silicone sponge is a closed cell silicone rubber.  It is an excellent material for applications that require a soft compressible material with a very low compression set.  Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless and non-toxic.  Silicone sponge rubber is most commonly red in color although it is also available in grey, black or white with a fine fabric finish on both sides.

Common Applications:

# Silicone sponge is an excellent material for gasketing applications that require a soft compressible material.  It can also be used for gaskets, seals, press pads, thermal insulating, thermal shielding, heat transfer, silk screening, print presses, and vibration mounts.

### TYPICAL PROPERTIES FOR AMS3195

| Property | Specification AMS3195 | Typical Values |
| --- | --- | --- |
| Density, lbs/cubic in. under ¼” thk. | .025 Max | .020 |
| Density, lbs/cubic in. over ¼” thk. | .020 Max | .018 |
| Compression Deflection, PSI | 6-14 | 11 |
| Compression set, 22 hrs @212(F | 60% Max | 5 |
| Brittle Point (F | -67 | -103 |
| Temperature Range (F | N/A | -103 to +450 |
| Water Absorption | 5% Max | Pass |
| Tensile Strength, PSI | N/A | 100 |
| Elongation % | N/A | 200 |

Available Industry Specifications:

AMS3195, Mil-R-46089, ASTM D1056, Mil-R-6130, Mil-Std 670

# Text boxes

Low Compression Set Medium Density

###### Closed Cell

Silicone Sponge